Text for specification

Description
flexible copper busbar, plain, insulated
6x 15.5 x 0.8
350 A, length 2 m
Accessories

Standards
IEC 61439-1:2011

Approvals
UL

Electrical data
Rated current (IEC):	350 A

power dissipation at full load of the item:	69.4 W

Miscellaneous 
The laminated Cu busbars considerably reduce the effort of connecting busbars. The bending devices required for solid copper busbars are unnecessary. The 2mm-thick insulation means that no additional covering is required.

Brand 
Woehner or equivalent

Part No.
01035000