Text for specification

Description
barramento 12 x 10
comprimento 2,40 m, estanhado
30Compact 3P
60Classic

Standards
IEC 61439-1:2011

Approvals
CSA, UL

Electrical data
power dissipation at full load of the item:	51,0 W

Rated current as per UL 150A
in 3-pole 60mm-System compact also 300A

Material properties
Main body:
	Cu-ETP R300 (EN 13601), tinned

corrosion-resistant, also in aggressive environments

Miscellaneous 
Tin-plated Cu busbars considerably reduce the effort of preparing the contact points.
The Cu busbars are effective protected against aggressive media.

Brand 
Woehner or equivalent

Nº da peça
01623000