Text for specification

Description
Cobertura de proteção IP20 (frontal)
incl. 3 coberturas da parte superior
300 mm largura
185Power

Standards
IEC 61439-1:2011

Electrical data

Material properties
Main body:
	temperature stability 125°C,
	self-extinguishing in acc. to UL 94,
	creepage resistance CTI 600,
	halogen-free
Cover:
	temperature stability 125°C,
	fire behaviour UL 94 HB,
	creepage resistance CTI 200,
	halogen-free 

Brand 
Woehner or equivalent

Nº da peça
32702000A