Text for specification

Description
barramento de cobre laminado, estanhado, isolado
6x 20 x 1
477 A, comprimento de 2 m
Accessories

Standards
IEC 61439-1:2011

Approvals
UL

Electrical data
Corrente de medição (IEC):	477 A

power dissipation at full load of the item:	79,9 W

Material properties
Insulation:
	temperature withstand up to 105 °C
	self-extinguishing, V0 according to UL 94
	breakdown voltage 20 kV
	stretching 370 %

Miscellaneous 
Tin-plated Cu bars considerably reduce the effort of preparing the contact points.
The Cu busbars are effectively protected against aggressive media.

Brand 
Woehner or equivalent

Nº da peça
01063000